## Slide 1: Finalized Commissioning of a Metal 3D-Printer; Validated Through Topology Optimization
Riley Shepard, Erik Leon, Sichao Jiang

## Slide 2: Project Description
Deliverables
Final Commissioning
  Validated printer and associated machines
  Software and hardware guides
  Tensile testing AM specimens- printer validation
  Train Idea Lab manager
Individual Design Projects
  Hip Abduction Bracket
  RC Excavator Arm
  RC Car Steering Knuckle
Service
  Optimize and manufacture for other capstones
Figure 1: Concept Laser MLab Cusing 100R
Riley, 1
Client: IDEA Lab and ME Department-Dr. Ciocanel
Budget: as needed
Impact: Expand NAU's manufacturing capabilities
Mentors: Mike Downey, Justin Sokel

## Slide 3: System Commissioning

## Slide 4: Printer Commissioning
Erik, 2
Results:
3 repaired modules
  2 functional, 1 fully validated
Working sieve unit
Parameters for printing in SS316 and Inconel 718
Operation manuals
Figure 2: Black Box Model and Functional Decomposition

## Slide 5: Partition
Propose Design (80/20)
  Confine printer and all related machines/materials
  Negative pressure
    Air flow kept within (CFD)
Approval From EHS
  Approval from building manager and fire department
Erik, 3
Figure 3: Partition Model
Figure 4: Simplified Partition
Figure 5: Partition CFD Simulation

## Slide 6: Printed Parts
Riley, 4
Figure 6: Gao Blocks and Mesh Ball
Figure 8: Hood Ornaments
Figure 7: Tensile Specimens

## Slide 7: Design Validation- FMEA
Erik, 5
Table 1: Printer FMEA

## Slide 8: Individual Design Projects

## Slide 9: Background and Benchmarking - RC Excavator
Background
RC Excavator Arm Segment(s)
Connects hydraulics to joints bucket
Optimization would decrease weight and/or increasing durability
Current design
  Plastic
  No 'speed holes'
Benchmarking
Example brackets from nTop and Ansys
Very similar to the stick portion of the excavator
Loading conditions will vary, but optimization should be similar
Figure 14: RC Excavator
Erik, 6
Figure 12: Density-based Topology Optimization
Figure 13: Static Load-based Topology Optimization

## Slide 10: Background and Benchmarking- Hip Abduction Bracket
Background
Allows hip abduction DOF
Necessary for functionality and comfort
Current design
Milled
~50g
~$500 per set
7075 T6 Al
Figure 9: Hip Exo- Highlighting Abduction Bracket
Benchmarking
[1] ] O. Okorie, et al.
Static topology optimization process of a bracket in Ansys
Shows initial design and multiple optimized models noting different constraints‌
[2] Nebojsa Raicevic et al.
Discusses parameters, constraints, and equations applied for a fatigue analysis and topology optimization for additive manufacturing
Riley, 7
Figure 10: Topology optimized aerospace bracket [1]
Figure 11: Topology optimized aerospace torque link [2]

## Slide 11: Background and Benchmarking -RC Steering Knuckle
Background
Function:
Supports the wheel axle and bearings
Connects suspension arm and steering link
Enables wheel steering motion
Design Requirements:
High stiffness and strength
Low weight for performance
Precise geometry for smooth steering
Benchmarking
Existing upgraded design: aluminum
Offers improved durability and steering precision
Compatible with performance suspension setups
Figure 15: Steering knuckle close-up
Sichao, 8
Figure 16: Steering knuckle CAD model

## Slide 12: Excavator Arm Design Requirements Summary
CR1: Safe for use
No risk of using
CR2: Lightweight
Can't tip excavator
CR3: Durable
Won't break while using
CR4: Functional
Excavator operates normally
ER1: Suitable Fit
Fits in initial assembly
ER2: Weight
Target: 10% weight reduction
ER3: Max Load
Target: 6.137x10^-4 Nm
ER4: Smooth Finish
Target: ~6.3μm
ER5: Range of Motion
Target: 10% longer than original
Erik, 9

## Slide 13: Hip Exo Design Requirements Summary
CR1- Lightweight Design
Necessary for exoskeletons
CR2- Durability/Reliability
Safe in long term use
CR3- Manufacturing Price
Reasonable cost for parts
CR4- Stable in Use
Safe operation
ER1- Weight Reduction
Target: 15% reduction
ER2- Lifetime
Target: 10^6 cycles
ER3- Manufacturing Cost
Target: <$500/set, <14 days
ER4- Safe Under Load
Load Case 1: Axial Load
Target: Safe for 0.72N load
Load Case 2: Bending Moment
Target: Safe for 0.0031Nm
Riley, 10

## Slide 14: Steering Knuckle Design Requirements Summary
CR1 – Lightweight Design
Minimize unsprung mass for better handling
CR2 – Durability / Reliability
Safe under repeated steering and driving loads
CR3 – Manufacturing Price
Reasonable cost for prototyping and production
CR4 – Stable Under Load
Maintain alignment and structural integrity during use
ER1 – Weight
Target: ≤ 20 g
ER2 – Lifetime
Target: ≥ 25,000 cycles
ER3 – Manufacturing Cost
Target: ≤ $80 / part
ER4 – Stable Axial Load Capacity
Target: Safe for 60 N axial load
ER5 – Stable Bending Moment Capacity
Target: Safe for 0.9 N·m bending moment
Sichao, 11

## Slide 15: Design Space Research

## Slide 16: Literature Review
[13] Mlab cusing R: Translation of Operating Manual, v1.0.15, CONCEPT Laser GmbH, 2013, S1 pp.10-141
[14] Instruction Manual: Wet Separator, v1.0.15, CONCEPT Laser GmbH, June 2014, S3 pp.7-39
[15] Mlab cusing: Concept Laser Software 1.2.4, v1.0.15, CONCEPT Laser GmbH, 2013, S4 pp.7-39
QM Powder: Automatic Sieving Station Operation Manual, v1.0.15, CONCEPT Laser GmbH, July 12, 2016. Accessed Sept. 16, 2025. [Online] Available: https://www.prestigeequipment.com/pix/29314.pdf
[16] nTop, “How to get the most out of topology optimization,” nTop, Mar. 19, 2020. https://www.ntop.com/resources/blog/how-to-get-the-most-out-of-topology-optimization/
[17] The Engineering Toolbox, “Young’s Modulus - Tensile and Yield Strength for common Materials,” Engineeringtoolbox.com, 2003. https://www.engineeringtoolbox.com/young-modulus-d_417.html
[18] R. M. Dhawale and S. R. Wagh, “FINITE ELEMENT ANALYSIS OF COMPONENTS OF EXCAVATOR ARM—A REVIEW,” Jan. 2014. https://www.ijmerr.com/v3n2/ijmerr_v3n2_40.pdf
[19] “Cleanroom,” Nau.edu, 2024. https://www.ceias.nau.edu/capstone/projects/ME/2024/F23toSp24_CleanRoom/
[20] “Fan Filter Unit (FFU),” Terrauniversal.com, 2025. https://www.terrauniversal.com/fan-filter-units.php (accessed Oct. 21, 2025).
[21] Specification for HEPA Filters Used by DOE Contractors. Washington, D.C. 20585: U.S. Department of Energy, 2005.
[22] T. H. Lee, J. Park, and S. Lee, “Lightweight design of steering knuckle using topology optimization and additive manufacturing,” Journal of Mechanical Science and Technology, vol. 34, no. 11, pp. 4425–4435, Nov. 2020. doi: 10.1007/s12206-020-0955-7.
‌
Riley, Erik, Sichao, 12
[1] O. Okorie, A. Perveen, D. Talamona, and K. Kostas, “Topology Optimization of an Aerospace Bracket: Numerical and Experimental Investigation,” Applied Sciences, vol. 13, no. 24, p. 13218, Jan. 2023, doi: https://doi.org/10.3390/app132413218.
[2] Nebojsa Raicevic, Aleksandar Grbović, Gordana Kastratović, Nenad Vidanović, and A. Sedmak, “Fatigue Life Prediction of Topologically Optimized Torque Link Adjusted for Additive Manufacturing,” International Journal of Fatigue, pp. 107907–107907, Aug. 2023, doi: https://doi.org/10.1016/j.ijfatigue.2023.107907.
[3] “Next-Gen Engineering Design Software: nTop (formerly nTopology),” nTop. https://www.ntop.com/
[4] P. Maggiore, S. Brischetto, and C. Ferro, Additive Manufacturing Technologies and Applications. 2017.
[5] D. Jankovics, H. Gohari, M. Tayefeh, and A. Barari, “Developing Topology Optimization with Additive Manufacturing Constraints in ANSYS®,” IFAC-PapersOnLine, vol. 51, no. 11, pp. 1359–1364, Jan. 2018, doi: https://doi.org/10.1016/j.ifacol.2018.08.340.
[6] “Design for Metal Additive Manufacturing Part 2: Topology Optimization and Build Preparation,” Ansys.com, 2023. https://www.ansys.com/academic/educators/education-resources/am-case-study-part-2 (accessed Sep. 15, 2025).
[7] “Safety management in metal Additive Manufacturing,” Metal Additive Manufacturing, Mar. 01, 2019. https://www.metal-am.com/articles/safety-management-in-metal-3d-printing/
[8] “Specification for Additive Manufacturing Stainless Steel Alloy (UNS S31603) with Powder Bed Fusion,” Sep. 2016, doi: https://doi.org/10.1520/f3184-16.
[9] ASTM International, “Test Methods for Tension Testing of Metallic Materials,” doi: https://doi.org/10.1520/e0008_e0008m-13a.
[10] E. Maleki, B. Salehnasab, M. Paul, S. Shao, and N. Shamsaei, “Dimensional accuracy of fabricated geometries through powder bed fusion: An overview and a new benchmark artifact proposal,” Materials & Design, vol. 257, p. 114361, Jul. 2025, doi: https://doi.org/10.1016/j.matdes.2025.114361.
[11] Georgi Genov, “REVISITING THE RULE-OF-THUMB DEPENDENCIES OF THE SHEAR STRENGTH AND THEHARDNESS ON THE YIELD AND THE ULTIMATE STRENGTHS,” Nov. 17, 2020.https://www.researchgate.net/publication/355208819_REVISITING_THE_RULE-OF-THUMB_DEPENDENCIES_OF_THE_SHEAR_STRENGTH_AND_THE_HARDNESS_ON_THE_YIELD_AND_THE_ULTIMATE_STRENGTHS
[12] “Metallurgy & Process Development – Castheon,” Castheon.com, 2025. https://www.castheon.com/process-material/metallurgy-and-print-parameter-development/ (accessed Oct. 08, 2025).​
[23] C. Wang, Y. Zhang, and H. Li, “Structural analysis and optimization of RC car steering knuckle under extreme cornering load,” International Journal of Vehicle Structures & Systems, vol. 12, no. 3, pp. 216–222, 2020.
Traxxas, Slash 2WD Exploded View & OEM Parts Manual, 2023. [Online]. Available: https://traxxas.com
[24] Integy RC, 6061-T6 Aluminum Steering Knuckle for Slash 2WD Product Sheet, 2023. [Online]. Available: https://www.integy.com
[25] S. K. Moon and Y. H. Kim, “Additive manufacturing of lightweight components for small-scale vehicles: steering system applications,” Rapid Prototyping Journal, vol. 28, no. 1, pp. 33–45, Jan. 2022.
[26] J. Thompson and R. D. Brandt, “Topology optimization for additive manufacturing using nTop Platform,” Additive Manufacturing Letters, vol. 3, pp. 100–108, 2021.
[27] nTop, nTop Platform Documentation and Tutorials, 2023. [Online]. Available: https://www.ntop.com
[28] ANSYS Inc., ANSYS Mechanical User’s Guide, 2023. [Online]. Available: https://www.ansys.com
[29] H. Zhang, Y. Sun, and K. Wang, “Mechanical Performance Optimization of Aluminum Suspension Components Using Additive Manufacturing,” Journal of Manufacturing Processes, vol. 85, pp. 1021–1032, 2023.
[30] A. Reeves and M. Patel, “Finite Element Analysis of RC Car Steering Knuckle Under Braking and Cornering Loads,” in Proc. Int. Conf. Vehicle Dynamics and Mobility, 2022, pp. 411–418.
[31] S. Müller, D. Koch, and T. Berg, “Design Verification of Additively Manufactured Ti-6Al-4V Components for Small Mechanical Assemblies,” Materials Today: Proceedings, vol. 72, pp. 554–562, 2024.
Riley:
Erik:
Sichao:

## Slide 17: RC Excavator Stick Mathematical Modelling & Engineering Calculations
Basic Static Finite Element Analysis
Applied Values:
Moment @ Bucket = .02Nm
Axial Force @ Bucket = .00091N
Results:
Max stress = ~3Pa
Max Displacement = 2.56e-7mm
Erik, 13
Figure 19: Excavator Stick FEA Results

## Slide 18: Hip Bracket Mathematical Modelling & Engineering Calculations
Basic Static FEA using Ntop
Applied values from MatMod Calculations
Results:
  Max Stresses:
    Hip Side: 49.56 kPa
    Motor Side: 360.87kPa
Riley, 14
Figure 18: Hip Bracket FEA Results
Known Parameters and Assumptions
Max Operational Torque at Motor:
  12 Nm
Known Distances:
  60mm- axis to axis
  44mm- motor axis to mounting screws
Alloy Steel M3 screws
Assumptions:
  Upright, carbon fiber motor brackets, and baseplate rigidly fixed
  All 4 bolts loaded equally
Results
  Will define boundary conditions for FEA and Top. Opt.
Equations
[11]
[11]
Figure 17: Hip Bracket Diagram

## Slide 19: Steering Knuckle Mathematical Modelling & Engineering Calculations
Steering Knuckle
Lateral static load at axle
L = 40 mm
F = 60 N
Critical section: Stepped hollow section
Material: 316 Stainless Steel
σy ≈ 205 MPa
Ix ≈ 6.35 × 10^2 mm^4
c ≈ 7.91 mm
Dominant mode: Bending
Stress concentration verified by FEA
Equation：
Results：
n=205/29.9≈6.9
Figure 22: Steering Knuckle Drawing
Sichao, 15
Figure 20: Steering Knuckle Static FEA
Figure 21: Steering Knuckle Displacement FEA
The maximum total displacement is approximately 9.49 × 10^-5mm
The maximum Von Mises stress is approximately 0.45 MPa
Basic Static Finite Element Analysis

## Slide 20: Concept Generation, Evaluation, & Selection

## Slide 21: Concept Generation, Evaluation, and Selection
Erik, 17
Table 3: Erik Concept Evaluation
Figure 24: Erik Concepts

## Slide 22: Concept Generation, Evaluation, & Selection- Riley
Riley, 18
Scoring Table |  |  |  | 
Criteria | Target | Hip Bracket | Toothed Bridge | Motor Mount
Topology Optimization Potential | High | High | Low | Moderate-Low
Post- Processing Requirements | Low | Low | Moderate | High
Fits within print volume | Yes | Yes | Yes | Yes
Visualization in Assembly | High | High | Moderate-Low | Low
Table 2: Riley Concept Evaluation
Figure 23: Riley Concepts

## Slide 23: Concept Generation, Evaluation, and Selection
Sichao, 19
Criteria | Basic magnetic hook | Pegboard power drill holder | RC car steering knuckle
Functional Complexity | Low | Moderate | High
Fit & Integration with Assembly | Moderate | High | High
Topology Optimization | Low | Moderate | High
Table 4: Sichao Concept Evaluation
Figure 25: Sichao Concepts

## Slide 24: Project Management

## Slide 25: Semester 1 GANTT Chart
Riley, 20
Figure 26: S1 GANTT Chart

## Slide 26: Semester 2 GANTT Chart
Riley, 21
Figure 27: S2 GANTT Chart

## Slide 27: Budget and BOM
Sichao, 22
Purchased:
23 of 23 items (100%)
On Hand：23 of 23 items (100%)
Remaining:
0 items
Figure 28: Purchasing Plan

## Slide 28: Optimization

## Slide 29: Engineering Calculations- Erik
Erik, 23
Applied boundary conditions used in FEA and a volume constraint of 0.5
Calculated new loads using actual dimensions
Excavator Arm
SS316L Ys = 170MPa
Max Stress = 0.031MPa
FoS = 5483
Figure 34: Optimized Stick FEA
Figure 35: Min/Max Stress
Figure 33: nTop Optimized Stick

## Slide 30: Excavator Stick Prototype
Erik, 24
Questions:
Does it fit?
  Connect to Bucket/Pins
  Connect to Boom
Methods:
3D printed in PLA
Answers:
Bucket: Yes
Pins: Yes
Boom: Yes
Next Steps:
Add additional necessary geometries
Topology optimize with a print-orientation parameter
Figure 36: Excavator Stick Prototype

## Slide 31: Engineering Calculations- Riley
Riley, 25
Topology Optimizations in nTop
Criteria:
Applied BCs used in FEA
Volume Constraint: 0.4
Symmetry Constraint
Figure 29: Topology Optimized Hip Side Bracket
Figure 30: Topology Optimized Motor Side Bracket
Max Stress Results:
0.205 MPa
0.289 MPa
Figure 31: Topology Optimized Hip Side Bracket

## Slide 32: Hip Abduction Bracket Prototype
Questions:
Does it fit?
  Bearings, shaft, bolts
Methods:
3D printed in PLA
Riley, 26
Answers:
Bearings fit
Shaft fits
ROM acceptable
Bracket hinges freely and smoothly
Improvements/Next Steps:
Topology optimize with a build orientation parameter & compare
Print bores undersized and post process to ensure proper press fit
Figure 32: Hip Side Bracket Prototype

## Slide 33: Engineering Calculations- Sichao
The maximum deformation is 0.00437 mm, which is very small.
The maximum equivalent stress is 122.58 MPa.
The maximum equivalent elastic strain is 7.59 × 10⁻⁴ .
The highest stress and strain are concentrated around the inner hole and curved transition area.
Figure 37: Steering Knuckle FEA
Sichao, 27

## Slide 34: Steering Knuckle Prototype
Questions:
Does it fit?
Wheel hub, bearings, kingpin screws
Steering link / tie-rod connection
Methods:
3D printed in PLA
Answers:
Fit: The connecting ball features need to be enlarged for a better connection
Surface: Needs Post-Processing
Next Steps:
Increase the size of the connecting ball features to improve assembly and connection performance
Sichao, 28
Figure 38: Steering Knuckle Prototype

## Slide 35: Active Rocket Control Lower Fin Arm-Service
Riley, 29
Original
Applied Force: 67N
Displacement Constraint around square bore
Max Stress: 9.96 MPa
Figure 39: ARC Original and Optimized FEA Results
Optimized
Max Stress Constraint: 17 MPa
Planar Symmetry Constraint
Key Geometries Reintroduced
Max Stress: 11.2 MPa

## Slide 36: Lerner Robotic Arm Hinge- Service
Riley, 30
Max Stress Constraint: 75 MPa
Volume Constraint: 0.5
Planar Symmetry Constraint
Key Geometries Reintroduced
Max Stress: 67.9 MPa
Figure 41: Topology Optimized FEA Results
Applied Force: 30 N
Applied Moment: 20Nm
Displacement Constraint around the 4 mounting holes
Max Stress: 44.95 MPa
Figure 40: Original Geometry FEA Results

## Slide 37: Lerner Robotic Arm Hinge- Service
Riley, 31
Original
Applied Force: 360 N
Displacement Constraint around bore
Max Stress: 35.28MPa
Figure 42: Hinge Stress FEA Results
Optimized
Max Stress Constraint: 50 MPa
Volume Constraint: 0.4
Key Geometries Reintroduced
Max Stress: 48.08 MPa

## Slide 38: Final Models

## Slide 39: Design Description- Erik
Erik, 33
Figure 45: Optimized Arm Assembly

## Slide 40: Design Description- Erik
Erik, 32
Figure 43: Excavator Arm Assembly
Figure 44: Topology Optimized Stick
Hollow Stick and Boom with rotating stick inside for movement

## Slide 41: Design Description- Riley
Design Functions
Provide powered assistance at the hip joint
Riley, 35
Figure 48: Hip Exo Assembly
Figure 49: Bracket Subassembly

## Slide 42: Design Description- Riley
Component Design Functions
Allows hip abduction and adduction DOF
Rigid connection between the hip belt to the motor
Riley, 36
Figure 50: Hip Side Bracket
Figure 51: Motor Side Bracket

## Slide 43: Design Description- Sichao
Sichao, 34
Steering Knuckle Assembly and Steering knuckle Design Drawings
The steering knuckle connects the wheel hub to the suspension and allows the wheel to turn with the steering system.
Figure 46: Steering Knuckle Assembly
Figure 47: Steering Knuckle

## Slide 44: Final Assemblies
Erik, 37
Final CAD Assemblies
  Erik- Excavator Arm
  Sichao- RC Steering Knuckles
  Riley- Hip Abduction Bracket
Figure 52: Excavator Final CAD
Figure 53: Steering Knuckle Final CAD
Figure 54: Hip Exo Final CAD

## Slide 45: Final Assemblies
Erik, 37

## Slide 46: Final Testing

## Slide 47: Excavator Arm Top Level Testing Summary
Experiment/Test | Relevant DRs | Testing Equipment | Other Resources
EXP1 - Comparison to Original | CR2 – Lightweight ER2 – 10-20% weight reduction ER5 – Range of Motion maintained | Scale Dial Caliper | Original Arm Optimized Arm
EXP 2 - Assembly | ER1 – Suitable fit ER4 – Smooth Finish | Boom and Bucket attachments | Screwdriver
EXP 3 – Run Excavator | CR1 – Functional CR4 – Safe for Use ER3 – Maximum torque of 6.137x10^-4 Nm | Excavator and Controller | Batteries Some material to scoop/dump
Table 5: Excavator Arm Top Level Testing
Erik, 38

## Slide 48: Hip Exo Top Level Testing Summary
Experiment/Test | Relevant DRs | Testing Equipment | Other Resources
EXP1- Mass Comparison | CR1- Lightweight ER1- Weight Reduction of 15% | Electronic Balance | Use arbor press to remove bearings
EXP 2- Manufacturing Cost Analysis | CR3- Manufacturing Cost ER3- Manufacturing Cost/Lead Time | Netfabb Slicer Printing Documentation Gas Consumption Documentation MATLAB | Create cost equations for printing based on volume and height of build
EXP 3- Static Loading Analysis | CR2- Durable ER2- Lifetime CR4- Stable in Use ER4- Axial Loading and Bending Moment | NTop CubeMars AK60 Spec Sheet | Analysis of loading conditions in nTop by resumulating topology optimized model
EXP 4- Qualitative Walk Test | CR4- Stable in Use ER4- Axial Loading and Bending Moment | Biomech Python GUI OpenExo Hip Exoskelton Laptop Treadmill | Assemble topology optimized bracket and complete overground and treadmill walking
Table 6: Hip Exo Top Level Testing
Riley, 39

## Slide 49: Steering Knuckle Top Level Testing Summary
Experiment / Test | Related Design Requirements (DRs) | Required Test Equipment | Other Resources
EXP1 – Mass Measurement Test | ER1 – Weight; CR1 – Lightweight | Gram scale | Final manufactured steering knuckle
EXP2 – Static Axial Load Test | ER4 – Stable Axial Load Capacity; CR2 – Durable; CR4 – Stable Under Load | Load fixture, force gauge | Mounted steering knuckle sample, test stand
EXP3 – Durability / Repeated Loading Test | ER2 – Lifetime; CR2 – Durable; CR4 – Stable Under Load | Assembled RC car, radio controller, battery, inspection tools | Flat test surface, completed steering system
EXP4 – Manufacturing Cost Evaluation | ER3 – Manufacturing Price; CR3 – Low Manufacturing Cost | Cost records, material pricing, manufacturing notes | Fabrication process documentation
Table 7: Steering Knuckle Top Level Testing
Sichao, 40

## Slide 50: Tensile Testing Summary
Experiment/Test | Relevant DRs | Testing Equipment | Other Resources
EXP1 – Tensile Tests | CR1 – SS316 CR2 – In 718 ER1 – SS316 UTS ≥ 480-620MPa, E ≥ 190-205GPa ER2 – In 718 UTS ≥ 965MPa, E ≥ 200GPa | 8802 Instron multiaxial testing machine | Lab Space Excel Spreadsheet ASTM E8/E8M Standards
Summary-
Follow ASTM E8/E8M standards to test all tensile specimens to failure while collecting displacement and force data
Experiment 1- Tensile Testing Details
Procedure-
Prepare the tensile specimens: organize & take measurements of the gauge length and gauge diameter
Set the speed of the machine based on strain rate limits  0.36 min^-1
Insert the specimen into the machine and clamp with the jaws
Preload and conduct the tensile test until part fracture
Repeat procedure for all tensile test specimens
Record all displacement and force data in an Excell spreadsheet
Complete calculations to obtain stress-strain data
Plot the stress-strain curve
Calculate the Elastic Modulus
Use the 2% Offset method to determine the yield stress
Report all results and compare to standard material properties
Results-
316L Material Properties
UTS ≥ 480 MPa
E ≥ 190GPa
Inconel 718 Material Properties
UTS ≥ 965 MPa
E ≥ 200 GPa
Table 8: Tensile Specimen Top Level Testing
Erik, 41

## Slide 51: Excavator Arm Specification Sheet ​
Engineering Requirement | Target | Tolerance | Measured / Calculated Value | Requirement Met? (✓ or X) | Customer Accepts? (✓ or X)
ER1 – Fit | Y | N/A | Y | ✓ | ✓
ER2 – Weight | 90% original | +/- 5g | 49.2g | X | ✓
ER3 – Max Load | 46g | + ∞ | > 46g | ✓ | ✓
ER4 – Surface | 6.3 μm | +/- 4 μm | > 6.3μm | X | ✓
ER5 – Range of Motion | 6.35cm | + ∞ | +0.05cm | ✓ | ✓
Customer Requirement | Requirement Met? (✓ or X) | Customer Accepts? (✓ or X)
CR1 – Safe | ✓ | ✓
CR2 – Lightweight | ✓ | ✓
CR3 – Durable | ✓ | ✓
CR4 – Functional | ✓ | ✓
Table 9: Excavator Arm EGR Specifications
Table 10: Excavator Arm Customer Specs.
Erik, 42

## Slide 52: Hip Exo Specification Sheet
Engineering Requirement | Target | Tolerance | Measured / Calculated Value | Requirement Met? (✓ or X) | Customer Accepts? (✓ or X)
ER1 –Lightweight | -15% of original | +/- 5% | Original vs. Topology Optimized: Al: -20% 316SS: -28.5% Actual: +56.9% | X | X
ER2 – Durable | -10 minutes of walking | +/- 1 minute | 10:48 minutes | ✓ | ✓
ER3 –Manufacturing Cost and Lead Time | <$500 <14 days | +/- $50 | Cost: $290.38 Min Days: 3 | ✓ | ✓
ER4 – Axial Load and Bending Moment | Withstand <9Nm motor torque | +/-0.5 FOS | Min: 588.23 | ✓ | ✓
Customer Requirement | Requirement Met? (✓ or X) | Customer Accepts? (✓ or X)
CR1 – Lightweight | X | X
CR2 – Durable | ✓ | ✓
R3 – Manufacturing Cost and Time | ✓ | ✓
CR4 – Stable in Use | ✓ | ✓
Table 11: Hip Exo EGR Specifications​
Table 12: Hip Exo Customer Specs.
Riley, 43

## Slide 53: Steering Knuckle Specification Sheet
Engineering Requirement | Target | Tolerance | Measured / Calculated Value | Requirement Met? (✓ or X) | Customer Accepts? (✓ or X)
ER1 – Weight | ≤ 20 g | N/A | 12g | ✓ | ✓
ER2 – Lifetime / Repeated Use Durability | No visible damage after repeated functional steering test | N/A | No visible damage | ✓ | ✓
ER3 – Stable Axial Load Capacity | ≥ 60 N | N/A | No visible damage | ✓ | ✓
ER4 – Manufacturing Price | ≤ $80 | N/A | $61.75 | ✓ | ✓
Customer Requirement | Requirement Met? (✓ or X) | Customer Accepts? (✓ or X)
CR1 – Lightweight | ✓ | ✓
CR2 – Durable | ✓ | ✓
CR3 – Stable Under Load | ✓ | ✓
CR4 – Low Manufacturing Cost | ✓ | ✓
Table 13: Steering Knuckle EGR Specifications
Table 14: Steering Knuckle EGR Specifications
Sichao, 44

## Slide 54: Tensile Testing Specification Sheet
Engineering Requirement | Target | Tolerance | Measured / Calculated Value | Requirement Met? (✓ or X) | Customer Accepts? (✓ or X)
ER1 – SS316 | UTS ≥ 480-620MPa E ≥ 190-205GPa | +/-0.5MPa +/-0.5GPa | 648.4MPa 56.GPa | ✓ X | ✓
ER2 – Inconel 718 | UTS ≥ 965MPa E ≥ 200GPa | +/-0.5MPa +/-0.5GPa | 1022 MPa 54.9 GPa | ✓ X | ✓
Customer Requirement | Requirement Met? (✓ or X) | Customer Accepts? (✓ or X)
CR1 – Print 316L SS | ✓ | ✓
CR2 – Print Inconel 718 | ✓ | ✓
Table 15: Tensile Specimen EGR Specifications
Table 16: Steering Knuckle Customer Specs.
Erik, 45

## Slide 55: Tensile Testing Results
Inconel 718
316L Stainless Steel
Figure 55: Stress v Strain
Erik, 46

## Slide 56: Tensile Testing
Figure 56: 8802 Instron
Erik, 47

## Slide 57: Future Efforts
Tune laser parameters further to improve overhang capabilities
  Upskin vs downskin
Validate all modules
Once partition approved, establish parameters and print in Titanium (Ti6Al4V)
Print parts for projects throughout NAU
Riley, 48

## Slide 58: Thank You
Questions?

## Slide 59: Appendix

## Slide 60: Excavator Arm Detailed Testing Plans
Summary-
Compare masses by disassembling excavator and weighing the original and optimized sticks
Measure the length of each stick and compare
Experiment 1 - Mass and Length Comparison
Procedure-
Use a dial caliper to measure the length (cm) of the original stick
Use a dial caliper to measure the length (cm) of the optimized stick
Compare the lengths to one another
Use a scale to measure the mass (g) of the original stick
Use a scale to measure the mass (g) of the optimized stick
Compare the lengths to one another
Results-
Goal: 10% decrease in mass compared to the original part
Expected: Optimized part will have higher mass
Result:
  Original:
    L = 11.53cm
    M = 13.3g
  Optimized:
    L = 11.55cm
    M = 49.2g
Riley, 39

## Slide 61: Excavator Arm Detailed Testing Plans
Summary-
Assemble the excavator using the optimized part
Experiment 2 - Assembly
Procedure-
Prepare all parts of the excavator for reassembly
Fit both halves of the optimized stick to the boom connection
Add all internal connectors to ensure the stick stays together
Add bucket connection, and screw together
Add bucket pins to connect the bucket’s hinge to the stick
Check for excessive friction and adjust accordingly
Results-
Goal: Excavator runs smoothly without issue
Expected: Based on all prototypes, the optimized part should fit and function
Result: Success!
Summary-
With fully assembled model, run it normally to verify everything works
Validates CR1: safe, CR3: durable, CR4: functional, and ER3: maximum load.
Experiment 3 – Run Excavator
Procedure-
Fully charge the excavator’s battery, and ensure the controller has power
Scoop a bucket-full of sand/dirt, and empty it 10x
Estimate weight using density and bucket volume
Scoop a bucket-full of rocks, and empty it 10x
Measure weight using a scale
Scoop an immoveable object to test for any sort of bending
Results-
Goal: Handles load and immoveable object with no bending
Expected: It is stainless steel. There is no chance
Result: Success!
Erik, 40

## Slide 62: Hip Exo Detailed Testing Plans
Summary-
Compare masses by disassembling the brackets and weighing each of the components
Comparison using software to compare weights across material
Experiment 1- Mass Comparison
Procedure-
Remove aluminum and topology optimized hip abduction brackets from exoskeletons
Disassemble the brackets, removing the pivots
Press the bearings out for both brackets.
Locate, turn on, and calibrate the electronic balance
Record measurement of the mass for each of the parts in a spreadsheet.
Collect mass properties in SolidWorks
Determine the percentage difference between the original and topology optimized parts
Results-
Decrease in mass of a minimum of 15% when comparing the original parts to the topology optimized parts
Printed part will have higher mass
Computational results will provide an accurate weight reduction
Summary-
Determine the difference between the monetary costs and lead times
Experiment 2- Manufacturing Cost Analysis
Procedure-
Record the time and gas consumption for printing the parts.
Record the height of the print in millimeters.
Record the volume of material printed using Netfabb Premium.
Convert the volume of material to mass of the metal powder used for the base plate and part model.
Complete calculations to estimate the cost of the materials and argon consumption.
Record the time it takes to go from a part model to the final part in hand
Results-
Reduction in total cost (material cost) and lead time when comparing conventional manufacturing from additive manufacturing
Below:
  $500
  14 days
Riley, 42

## Slide 63: Hip Exo Detailed Testing Plans
Summary-
Limited by timeline and testing fixtures
Use software to validate safety factors under expected maximum loading scenario
Experiment 3- Static Loading Analysis
Procedure-
Import topology optimized model back into nTop
Mesh the model
Apply the 316L SS material model
Apply all boundary and loading conditions
Run the simulation
Read and report the maximum stresses
Calculate the factor of safety using the maximum stress of the result and the yield stress of the material
Results-
Based on static loading analysis:
  Safe use- minimum FOS of 2
  Durability- minimum FOS of 10
Summary-
Evaluate parts’ ability to withstand the expected loading conditions under a light number of cycles
Experiment 4- Exoskeleton Walk Test
Procedure-
Disassemble one side of the hip exoskeleton to remove the hip abduction bracket
Install the topology optimized hip abduction bracket on the exoskeleton
Power up the exoskeleton, complete calibration protocols, and set a torque setpoint of 9Nm
Complete walking overground throughout the LRC and outside on south campus of NAU.
Complete treadmill walking at 1.25m/s
Record all observations throughout the walk test
Results-
verification of hinge function for multiple walking conditions
stable operation of the topology optimized hinge
Riley, 43

## Slide 64: Steering Knuckle Detailed Testing Plans
Summary- • Verify that the final steering knuckle meets the weight requirement • Evaluate lightweight performance for the RC car suspension and steering system
Procedure-
Place the digital scale on a level surface
Turn on the scale and zero it properly
Clean the steering knuckle before measurement
Place the finished steering knuckle on the scale
Record the mass in grams
Repeat the measurement three times
Calculate the average mass
Compare the average value to the 20 g target
Experiment 1 – Mass Measurement
Results- • Average mass should be less than 20 g • Confirms the lightweight requirement is satisfied • Supports ER1 and CR1
Summary- • Evaluate whether the steering knuckle remains stable under axial loading • Check for cracking, yielding, or permanent deformation under the design load
Procedure-
Mount the steering knuckle in a representative test fixture
Align the applied force with the axial loading direction
Zero the force gauge or testing machine
Apply the load gradually in increments
Increase the load until it reaches 60 N
Observe deformation or cracking during loading
Hold the full 60 N load for 10–30 seconds
Remove the load and inspect the part
Experiment 2 – Static Axial Load Test
Results- • The steering knuckle should survive 60 N without fracture • No unacceptable permanent deformation should occur • Confirms ER4 and supports CR2 and CR4
Sichao, 45

## Slide 65: Steering Knuckle Detailed Testing Plans
Summary- • Perform a practical durability evaluation using the assembled RC car • Verify that the steering knuckle remains functional after repeated steering motion
Procedure-
Install the steering knuckle into the front steering assembly
Confirm normal steering operation before testing
Place the RC car on a flat test surface
Repeatedly steer from left lock to right lock and back
Count each full steering motion as one cycle
Perform approximately 200 to 500 cycles
Inspect the part every 50 to 100 cycles
Check for cracks, looseness, wear, or permanent deformation
Perform a final inspection after testing
Experiment 3 – Durability / Repeated Loading Test
Results- • No visible cracks should appear • No permanent deformation should be observed • Steering should remain smooth and functional • This serves as a prototype-level durability screening test
Summary- • Determine whether the steering knuckle can be manufactured at acceptable cost • Compare the total manufacturing cost to the target value
Procedure-
Record the amount of material used for one part
Determine the material cost
Record machine or fabrication cost
Record post-processing cost
Add all cost components together
Calculate the total manufacturing cost per part
Compare the final value to the $80 target
Experiment 4 – Manufacturing Cost Evaluation
Results- • Total manufacturing cost should be less than or equal to $80 per part • Confirms the design remains economical for prototyping • Supports ER3 and CR3
Sichao, 46